## Slide 1
Introduction to Database File (tdb)
June 2015
CompuTherm, LLC, Madison, Wisconsin, USA http://www.computherm.com
Part 1

## Slide 2: Element
Element Zn HCP_A3 65.39 5656.7 41.631 !
keyword
element name
structure
atomic weight
(g/mol)
H298
S298
Note
Pandat has a built-in table of atomic weights of elements.
If a compound (e.g., Al2O3) is defined as an element, its atomic weight has to be specified in the definition.
Pandat does not use structure, H298 and S298 in current version.
end of definition

## Slide 3: Function
Function GHCPAl 298.15 5481-1.8*T+GHSERAl; 6000 N !
keyword
function name
temperature range
temperature range
end of function
end of definition
function expression
5481-1.8T +

## Slide 4: Function (multiple ranges)
Function GHSERAl 298.15 -7976.15+137.072*T-24.3672*T*ln(T)
-0.00188466*T**2-8.77664e-007*T**3+74092*T**(-1); 700 Y
-11276.2+223.027*T-38.5844*T*ln(T)
+0.018532*T**2-5.76423e-006*T**3+74092*T**(-1); 933.6 Y
-11277.7+188.662*T-31.7482*T*ln(T)
-1.23426e+028*T**(-9); 2900 N !
temperature range
continued
keyword
function name
range 1
range 2
range 3

## Slide 5: Type Defintion
Type_Definition a GES A_P_D FCC_A1 Magnetic -3 0.28!
keyword
data-type code
keyword
append
phase
description
phase name
property
f
p
p : the fraction of the magnetic enthalpy absorbed above the critical temperature, depends on the structure
P(BCC_A2) = 0.40
P(!BCC_A2) = 0.28
f : a magnetic factor for Tc<0 and Bmag<0
if (Tc<0) then Tc/f → Tc and Bmag/f → Bmag

## Slide 6: Species
keyword
species
name
definition
Species Al2O3 Al2O3 !
keyword
species
name
definition
Species CuO Cu1O1 !

## Slide 7: Phase
Phase Liquid % 1 1 !
keyword
phase
name
number of
sublattices
sublattice size

## Slide 8: Constituent
Constituent Liquid :Al,Mg,Zn:!
keyword
phase
name
constituents on sublattice

## Slide 9: Parameter
Phase Liquid % 1 1 !
Constituent Liquid :Al,Mg,Zn:!
Parameter G(Liquid,Al;0) 298.15 +GLIQAl; 3000 N !
keyword
constituent
Phase name
type
power index
of interaction
function
GLIQAl
where

## Slide 10: Parameter
Phase Liquid % 1 1 !
Constituent Liquid :Al,Mg,Zn:!
Parameter G(Liquid,Al,Zn;1) 298.15 -810+0.471*T; 6000 N !
keyword
constituents
Phase name
type
power index
of interaction
function
-810+0.471*T
where

## Slide 11: Parameter
Parameter G(Liquid,Al,Mg,Zn;0) 298.15 -4094.48; 6000 N !
Parameter G(Liquid,Al,Mg,Zn;1) 298.15 -39973.7; 6000 N !
Parameter G(Liquid,Al,Mg,Zn;2) 298.15 -11337.5; 6000 N !
-
-
-
()
where
and

## Slide 12: Parameter
Phase BCC_A2 %c 1 1 !
Constituent BCC_A2 :Al,Mg,Zn:!
Parameter G(BCC_A2,Al;0) 298.15 +GBCCAl; 6000 N !
Parameter G(BCC_A2,Mg;0) 298.15 3100-2.1*T+GHSERMg; 6000 N !
Parameter G(BCC_A2,Zn;0) 298.15 +GBCCZn; 6000 N !
Parameter G(BCC_A2,Al,Zn;0) 298.15 20000; 6000 N !
+
+
+
where

## Slide 13: Parameter
Phase SIGMA % 2 0.66667 0.33333 !
Constituent SIGMA :Al,Zn:Mg:!
Parameter G(SIGMA,Al:Mg;0) 298.15 20133.7+6.3946*T +0.66667*GLIQAl+0.33333*GLIQMg; 3000 N !
Parameter G(SIGMA,Zn:Mg;0) 298.15 -19389.7+13.644*T +0.66667*GLIQZn+0.33333*GLIQMg; 3000 N !
Parameter G(SIGMA,Al,Zn:Mg;0) 298.15 -26000; 3000 N !
Parameter G(SIGMA,Al,Zn:Mg;1) 298.15 9335.47; 3000 N !
+
where

## Slide 14
For any questions and comments, contact CompuTherm by email:
info@computherm.com